## Use of UTEVA for the separation of Th, U, Np and Pu

N. Vajda, Zs. Molnár, Sz. Osváth

EiChrom Users’ Group Meeting

7 June 2002

Determination of distribution coefficients

Higher distribution ratios can be achieved from HCl acid but Np retention is suppressed by Fe complexes as it is revealed by the kinetic studies.

It is likely that Np exists as tetravalent complex in 9M HCl.

The retention of Np in all oxidation states is improved by the presence of iron(III) nitrate salting out agent in 8M HNO3. It is likely that Np prevails as penta and hexavalent nuclide in concentrated nitric acid.

Elution chromatographic studies

Columns were prepared from 0,5g of soaked UTEVA, column length was 34 mm.

Elution sequence:

1st load

2nd elution: with the same solution as during loading

3rd elution: 8 M HNO3 and/or 9M HCl

4th Pu strip: 0.1M NH4I/9M HCl

5th Np/Th strip: 4M HCl

6th U strip: 0.1M HCl

## Separations in 9M HCl

Only possible if no Fe is present in the load solution.

In this case, Np probably as Np(IV) is well separated from the matrix and other actinides except Th.

To determine the mechanism of the process tests were performed from the same load solution paralell with anion exchange resin (Bio Rad AG 1x8) column of the same size. It was supposed that only tetravalent Np is retained on the ion exchanger.

Separation of actinides from HCl can be performed in special samples of low Fe content:

e.g. separation and analysis of actinides from irradiated uranium

## Separations in 8M nitric acid

Without oxidation state adjustment Np exists in different forms, appearing in 2 elution peaks in the chromatogram:

Hexavalent Np is prepared by boiling with KBrO3 or KMnO4 in 1M HNO3

Pentavalent Np is prepared by the addition of NaNO2.

### To study the retention mechanism aliquots of the load solution were passed through UTEVA and Bio Rad AG 1*8 columns.

Np is retained by the UTEVA as pentavalent and hexavalent complexes while tetravalent is preferred by the anion exchangers.

The behaviour of Pu, U and Np was tested under the same conditions as that of Np.

100 ml of load solutions were prepared supposing that samples cannot be dissolved in small amounts of solutions.

Pu, Th/Np and U strip solutions were analysed for all nuclides by preparing alpha sources -under reductive conditions- using NdF3 for micro-coprecipitation.

## Analysis of standard reference materials

Modelling environmental samples

Unfortunatelly, there are no SRMs for 237Np.